Sujeto a  Requisitos:

8.2 Los requisitos básicos son siempre en vigor, salvo que sea reemplazada por el sujeto a  requisitos específicos en la "línea de call-out.”

| Requisitos básicos y el primer sujeto a N º |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Basic | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 |
| Requirement or |  |  |  |  |  |  |  |  |  |  |
| Suffix Letter |  |  |  |  |  |  |  |  |  |  |
| Tensile Strength, | D 412, | ... | ... | ... | ... | ... | ... | ... | ... | ... |
| Elongation | die C |  |  |  |  |  |  |  |  |  |
| Durometer Hardness, | D 2240 | ... | ... | ... | ... | ... | ... | ... | ... | ... |
| Type A |  |  |  |  |  |  |  |  |  |  |
| Suffix A, Heat | ... | D 573, 70 h | D 865, 70 h | D 865, 168 h | D 573, 168 h | D 573, 1000 h | D 865, 1000 h | ... | ... | ... |
| Resistance |  |  |  |  |  |  |  |  |  |  |
| Suffix B, Compression | ... | D 395, 22 h, | D 395, 70 h, | D 395, 22 h, | D 395, 70 h, | D 395, 1000 h, | D 395, 1000 | ... | ... | ... |
| Set, Standard Test |  | Method B, | Method B, | Method B, | Method B, | Method B, | h, Method B, |  |  |  |
| Specimen Cut from a |  | solid | solid | plied | plied | solid | plied |  |  |  |
| Slab |  |  |  |  |  |  |  |  |  |  |
| Suffix C, Ozone or | ... | D 1171, | D 1171,B | D 1171, | ... | ... | ... | ... | ... | ... |
| Weather Resistance |  | ozoneA | weather | ozoneC |  |  |  |  |  |  |
|  |  | exposure, |  | exposure, |  |  |  |  |  |  |
|  |  | Method A |  | Method B |  |  |  |  |  |  |
| Suffix D, | ... | D 575, | D 575, | ... | ... | ... | ... | ... | ... | ... |
| Compression- |  | Method A | Method B |  |  |  |  |  |  |  |
| Deﬂection Resistance |  |  |  |  |  |  |  |  |  |  |
| Suffix EO, Oil | ... | D 471, ASTM | D 471, ASTM | D 471, ASTM | D 471, ASTM | D 471, ASTM | D 471, ASTM | D 471, | D 471, |  |
| Resistance |  | Oil No. 1,D | Oil No. 2D , | Oil No. 3D , | Oil No. 1, | Oil No. 2, | Oil No. 3, | Service | Oil as |  |
|  |  | 70 h | 70 h | 70 h | 168 h | 168 h | 168 h | Liquid No. | speciﬁcally |  |
|  |  |  |  |  |  |  |  | 101, 70 h | designated |  |
|  |  |  |  |  |  |  |  |  | in Table 6, |  |
|  |  |  |  |  |  |  |  |  | 70 h |  |
| Suffix EO, Oil Resistance | ... | D 471, ASTM Oil No. 1,D 70 h | D 471, ASTM Oil No. 2D , 70 h | D 471, ASTM Oil No. 3D , 70 h | D 471, ASTM Oil No. 1D , 168 h | D 471, ASTM Oil No. 2D , 168 h | D 471, ASTM Oil No. 3D , 168 h | D 471, Service Fluid No. | D 471, Oil as speciﬁcally |  |
|  |  |  |  |  |  |  |  | 101, 70 h | designated |  |
|  |  |  |  |  |  |  |  |  | in Table 6, |  |
|  |  |  |  |  |  |  |  |  | 70 h |  |
| Suffix EF, Fluid | ... | D 471, Refer- | D 471, Refer- | D 471, Refer- | D 471, Refer- | D 471, Vol | ... | ... | ... | ... |
| Resistance |  | ence Fuel A, | ence Fuel B, | ence Fuel C, | ence Fuel D, | ume Percent |  |  |  |  |
|  |  | 70 h | 70 h | 70 h | 70 h | Reference |  |  |  |  |
|  |  |  |  |  |  | Fuel D Plus |  |  |  |  |
|  |  |  |  |  |  | 15 Volume |  |  |  |  |
|  |  |  |  |  |  | Percent |  |  |  |  |
|  |  |  |  |  |  | Denatured |  |  |  |  |
|  |  |  |  |  |  | Ethanol, 70 h |  |  |  |  |
| Suffix EA, Aqueous | ... | D 471, Dis- | D 471, Equal | ... | ... | ... | ... | ... | ... | ... |
| Fluid Resistance |  | tilled Water, 70 hE | Parts by Volume Distilled |  |  |  |  |  |  |  |
|  |  |  | Water-Reagent |  |  |  |  |  |  |  |
|  |  |  | Grade Ethylene Glycol, 70 hF |  |  |  |  |  |  |  |
| Suffix F, Low | ... | D 2137, | D 1053, 5 min, | D 2137, | D 1329, 38.1 | D 1329, 38.1 |  |  |  | ... |
| Temperature Resistance |  | Method A, 9.3.2, 3 min | T2,T5,T10,T50, or T100 | Method A 9.3.2, 22 h | mm die, 50 % elongation, retraction | mm die, 50 % elongation, retraction |  |  |  |  |
|  |  |  |  |  | 10 % min | 50 % min |  |  |  |  |
| Suffix G, Tear | ... | D 624, die B | D 624, die C | ... | ... | ... | ... | ... | ... | ... |
| Resistance |  |  |  |  |  |  |  |  |  |  |
| Suffix H, Flex | ... | D 430, | D 430, | D 430, | ... | ... | ... | ... | ... | ... |
| Resistance |  | Method A | Method B | Method C |  |  |  |  |  |  |
| Suffix J, Abrasion | ... | G | ... | ... | ... | ... | ... | ... | ... | ... |
| Resistance |  |  |  |  |  |  |  |  |  |  |
| Suffix K, Adhesion | ... | D 429, | D 429, | Bond made | ... | ... | ... | ... | ... | ... |
|  |  | Method A | Method B | after |  |  |  |  |  |  |
|  |  |  |  | vulcanization |  |  |  |  |  |  |
| Suffix K, Adhesion | ... | D 429, Method A | D 429, Method B | Bond made after vulcanizationG | ... | ... | ... | ... | ... | ... |
| Suffix M, Flammability | ... | ... | ... | ... | ... | ... | ... | ... | ... | ... |
| ResistanceG |  |  |  |  |  |  |  |  |  |  |
| Suffix N, Impact | ... | ... | ... | ... | ... | ... | ... | ... | ... | ... |
| ResistanceG |  |  |  |  |  |  |  |  |  |  |
| Suffix P, Staining | ... | D 925, | D 925, Method | ... | ... | ... | ... | ... | ... | ... |
| Resistance |  | Method A | B Control Panel |  |  |  |  |  |  |  |
| Suffix R, Resilience | ... | D 945 | ... | ... | ... | ... | ... | ... | ... | ... |
| Suffix Z, Special | ... | ... | ... | ... | ... | ... | ... | ... | ... | ... |
| RequirementG |  |  |  |  |  |  |  |  |  |  |
| Suffix Z, Special RequirementH | ... | ... | ... | ... | ... | ... | ... | ... | ... | ... |